Appendix A. Supplementary data

Enhancement in Carbon Dioxide Reduction Activity and Stability on Nanostructured Silver Electrode and the Role of Oxygen

Michael Shincheon Jeea,b, Hyo Sang Jeona,c, Cheonghee Kima, Hangil Leed, Jai Hyun Koha, Jinhan Chob, Byoung Koun Mina,c,e*, and Yun Jeong Hwanga,c*

a Clean Energy Research Center, Korea Institute of Science and Technology, 39-1 Hawolgok-dong, Seongbuk-gu, Seoul 136-791, Republic of Korea.

b Department of Chemical and Biological Engineering, Korea University, Anam-dong, Seongbuk-gu, Seoul 136-713, Republic of Korea.

c Korea University of Science and Technology, 217 Gajungro, Yuseong-gu, Daejeon 305-350, Republic of Korea.

d Department of Chemistry, Sookmyung Women’s University, Seongpa-dong 2-ga, Youngsan-gu, Seoul 140-742, Republic of Korea

e Green School, Korea University, Anam-dong, Seongbuk-gu, Seoul 136-713, Republic of Korea.

* Corresponding authors at: Clean Energy Research Center, Korea Institute of Science and Technology, 39-1 Hawolgok-dong, Seongbuk-gu, Seoul 136-791, Republic of Korea.

Tel.: +82 2 958 5853; fax: +82 2 958 5809

E-mail addresses: bkmin@kist.re.kr (B. K. Min), yjhwang@kist.re.kr (Y. J. Hwang)

Table S1. Summary of morphological and electrochemical properties of Ag foil and p-Ag samples.

| Sample | Particle Size [nm] | Roughness Factor | Oxygen Conc. [at.%] | Δη at 10 mA cm–2 [mV] | CO Tafel Slope [mV dec–1] | Exchange jCO [mA cm–2] |
| --- | --- | --- | --- | --- | --- | --- |
| Ag foil | n/a | 1.00 | 22.5 | 0a) | 148 | 2.73 × 10–6 |
| p-Ag:1 | 142±44 | 7.65 | 25.3 | 150 | 147 | 9.72 × 10–5 |
| p-Ag:5 | 104±33 | 4.15 | 20.0 | 160 | 143 | 1.05 × 10–5 |
| p-Ag:50 | 41±11 | 2.38 | 19.7 | 80 | 141 | 5.23 × 10–6 |
| p-Ag;200 | 28±7.6 | 1.72 | 19.8 | 120 | 140 | 4.70 × 10–6 |

a)η = 1050 mV

Figure S1. (a-d) Cyclic voltammograms of p-Ag:1, p-Ag:5, p-Ag:50, and p-Ag:200. (e) Charges passed at the last half of the fifth scan. Negative charges represent charges flown cathodically.

Figure S2. SEM images of (a) untreated Ag foil, (b) p-Ag:1, (c) p-Ag:50, and (d) p-Ag:200 samples after CO2RR for 2.5 h, respectively.

Figure S3. ECSA measurement of Ag foil and p-Ag samples using underpotential deposition (UPD) of Pb. Cyclic voltammetry voltammogram showing the UPD and bulk deposition of Pb onto Ag foil and p-Ag samples. The cathodic peak at -0.30 vs. Ag/AgCl is attributed to the Pb UPD and the corresponding charges tend to increase with decreasing scan rate.

Figure S4. Tafel plots of Ag foil and p-Ag samples showing similar Tafel slopes.

Figure S5. 13C isotope chromatograms confirms C source to be from dissolved CO2.